## TECHNICAL DATA SHEET

SINGLE CORE

THIN WALL MARINE CABLES

Profile:

Thin Wall low voltage tinned copper multicore wiring cables suitable for use in the marine industry. Resistant to petrol, diesel, lubricating oils and diluted acids.

Suitable for use at temperatures up to 105°C.

Insulation Properties:

Calcium Zinc based insulation compound to ISO6722-2000 Class B

Tensile Strength			24.0 N/mm²

Elongation at break			300%

Shore “D” Hardness:			56 @ 15 secs

Specific Gravity				1.34g/cc

Thermal Stability			200 mins @ 200°C

# Sheath Properties

Easy tear PVC sheathing to BS7655 Type 6

Tensile Strength			9.0 N/mm²

Elongation at break			260%

Shore “A” Hardness			79

Specific Gravity				1.60g/cc

BS Softness				36

Thermal Stability			70 mins @ 200°C

COPPER STRAND PROPERTIES

Tinned Copper wires conforming to BS EN 60228

Part No.	Copper	Cross			Current		Overall

Section		Rating	           	Dim’ns

(mm)		 	(amps)			(mm)

CM1.5 		21/0.30	   	1.5			21.0			2.4

CM2.5 	  	35/0.30	   	2.5			29.0			3.0

CM4.0 		56/0.30	   	4.0			39.0			3.7

CM6.0 		84/0.30	   	6.0			50.0			4.3

CM10.0		80/0.40	   	10.0			70.0			6.0